## Slide 1
ThinFilm | Film Thickness Monitor Calibration
Solutions | 
www.thinfs.com | Providing Innovation in Thin Films
How to Calibrate the Tooling Factor (2): Multi-Layer Method
The Half-Wave Ripple Test
Calibrates TWO materials at same time.
Deposits similar thickness to process.
Deposits stack under process conditions.
Can be analysed by simple spreadsheet.

## Slide 2
ThinFilm | Film Thickness Monitor Calibration
Solutions | 
www.thinfs.com | Providing Innovation in Thin Films
How to Calibrate the Tooling Factor (2): Multi-Layer Method
The Half-Wave Ripple Test:- (1H 2L 2H 2L 2H 2L 1H)
Centre- wavelength
Min-1
Min-2

## Slide 3
ThinFilm | Film Thickness Monitor Calibration
Solutions | 
www.thinfs.com | Providing Innovation in Thin Films
How to Calibrate the Tooling Factor (2): Multi-Layer Method
TiO2: 5% thin
SiO2: 5% thick

## Slide 4
ThinFilm | Film Thickness Monitor Calibration
Solutions | 
www.thinfs.com | Providing Innovation in Thin Films
How to Calibrate the Tooling Factor (2): Multi-Layer Method
TiO2: 5% thick
SiO2: 5% thin

## Slide 5
ThinFilm | Film Thickness Monitor Calibration
Solutions | 
www.thinfs.com | Providing Innovation in Thin Films
How to Calibrate the Tooling Factor (2): Multi-Layer Method
Ta2O5/SiO2
TiO2/SiO2

## Slide 6
ThinFilm | Film Thickness Monitor Calibration
Solutions | 
www.thinfs.com | Providing Innovation in Thin Films
How to Calibrate the Tooling Factor (2): Multi-Layer Method