## Slide 1
Motorized directional reflectance / transmittance analyser

## Slide 2
intermediate
MAC_trigger.exe
Motorized Accessory Controller interface - MAC2002

## Slide 3: Features
Absolute measurement of reflectance and transmittance
BRDF/BTDF measurements (angular resolved scattering)
Fully automated
Proper detection of secondary beams coming from the back of the sample and inter-reflections
Double beam advantage (reproducability < 0.05%)
Accurate (< 0.2% in UV/Vis range, < 0.4% in NIR range up to 2000nm and 0.6% between 2000 nm and 2500 nm))
Uncertainty in the angular settings < 0.023 degrees
Adjustable sample spot size ( 2 – 10 mm )
Incident beam angle +/- 180 degrees adjustable
Detection angle adjustable in the range 15 – 345 degrees
Polarisation degree adjustable between P and S
Wavelength range 250 nm – 2,500 nm (with larger integration times < 280 nm and > 2000 nm)

## Slide 4: Main applications
Absolute measurement of directional reflectance and transmittance of specular samples
Optical characterisation of coatings e.g. coating thickness, optical constants of individual layers in multi-layer coatings
Measurement of color shift as function of the angle of incidence
BRDF (Bidirectional Reflectance diffuse function) measurements (Angula resolved scattering) on diffuse samples (also BTDF capability)

## Slide 5
substrate / 62.2 nm TiO2 / 12.6 nm Cr / 42.3 nm TiO2
transmittance
front reflectance
back reflectance

## Slide 6: Optical constants determined with the TNO coating analyser
63.3 nm TiO2
42.3 nm TiO2
12.6 nm Cr
2 mm window glass
n
n
k
k

## Slide 7
substrate / HfO2 / SiO2 / HfO2 / SiO2 / HfO2 / SiO2

## Slide 8
210.6 nm HfO2
64.4 nm SiO2
2 mm Suprasil
n
n
k=0
k=0
188.8 nm HfO2
196.3 nm SiO2
28.6 nm HfO2
195.6 nm SiO2

## Slide 9
ellipsometry
photometry
Accuracy in the measurement

: 0.2%
-
0.3%

: 0.2%
-
0.5%
R, R': 0.2%
-
0.5%
T: 0.1%
-
0.3%
sensitivity for layer thickness
d < 5 nm
5 nm < d < 500 nm
d > 500 nm
++
++
+
+
++
++
Sensitivity for optical constants
n
low k
high k
++
-
++
++
++
++
Information content
+
+
+++
flexibility
+
+++
performance / price ratio
+
++
Ellipsometry versus Photometry (directional RT)
Notes: <number>
<footer>
<header>
<date/time>

## Slide 10
Angular resolved scattering measurements on diffuse samples
(example : 2mm window glass, one side sandblasted)
550 nm
Intensity

## Slide 11
The entrance port of the integrating sphere detector is equipped
with a variable slit to set a well defined acceptance angle
Slit adjustment
Entrance port

## Slide 12
PE Part number
URA
automated R/T
analyser 2)
L6310201
L6310201 or
L6310205
3)
IV Reflectance
accessory 2)
Absolute measurement
+
+
-
+
+
Directional Reflectance
+
+
+
+
+
Directional transmittance
-
+
+
-
-
BRDF/BTDF
1)
-
+
-
-
-
angle of incidence
8

- 68

0°-85° (T)
7.5°-85° (R)
15° - 355° (ARS) 1)
0°-80° (T)
15°-75° (R)
8° - 75°
6° - 80°
accuracy
+
++
+++
++
+++
Low reflectance samples
+
+
-
-
-
Laser mirrors
-
-
-
+
++
coating analysis
+
++
++
+
+
angular resolved scattering
-
+
-
-
-
Overview
Applications
+